

Submittal Information

CPVC End Caps

F

* Standard Size End Caps Fabricated From Seamless

Extruded CPVC Duct

* End Caps Are Triple-Pass Welded Using 5/32” CPVC

Welding Rod

\*Depending on Size, End Caps May Have 1-2 Seams

* All Dimensions are in Inches
* All Dimensions are to CSSI Standards and are Subject to Change

PRODUCT DIMENSIONS

|  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|

|  |  |  |  |  |
| --- | --- | --- | --- | --- |
|

|  |
| --- |
|  |
|  |
|  |
|  |

 |
|  |
|

|  |
| --- |
|  **ALL DIMENSIONS ARE TO CSSI STANDARDS AND ARE SUBJECT TO CHANGE** |

 |

|  |
| --- |
|  |

 |

 CPVC END CAPS SUBMITTAL INFORMATION

Model Number Nominal Duct Size Average Duct O.D. Average Wall Thickness A Length

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |
|  CA-CPVC-6 | 6 | 6.625 | 0.187 | 6.625 + 1/16 | 3.25 |
|  CA-CPVC-7 | 7 | 7.375 | 0.187 | 7.375 + 1/16 | 3.25 |
|  CA-CPVC-8 | 8 | 8.625 | 0.187 | 8.625 + 1/16 | 3.25 |
|  CA-CPVC-9 | 9 | 9.375 | 0.187 | 9.375 + 1/16 | 3.25 |
|  CA-CPVC-10 | 10 | 10.75 | 0.187 | 10.75 + 1/16 | 3.25 |
|  CA-CPVC-12 | 12 | 12.75 | 0.187 | 12.75 + 1/16 | 3.25 |
|  CA-CPVC-14 | 14 | 14 | 0.187 | 14 + 1/16 | 3.25 |
|  CA-CPVC-16 | 16 | 16 | 0.187 | 16 + 1/16 | 3.25 |
|  CA-CPVC-18 | 18 | 18 | 0.187 | 18 + 1/16 | 3.25 |
|  CA-CPVC-20 | 20 | 20 | 0.219 | 20 + 1/16 | 3.25 |
|  CA-CPVC-24 | 24 | 24 | 0.25 | 24 + 1/16 | 3.25 |